Mirror Finish Specifications (Metric)

Issue Date: 7/11/2012     Revision Date: 7/11/2012          Page 1 of 1          Approval: David Beickelman

| # Characteristic | # Specification |
| --- | --- |
| ## Scratches | # Acceptable |
| Under 1.5 mm |  |
| 1.5 mm – 12.7 mm | 1 per 30 cm x 30 cm area |
| Over 12.7 mm | # None |
| ## Pits and Speckles |  |
| # < 0.5 mm | Acceptable |
| .53 mm to 1.25 mm | 8 per 30 cm x 30 cm area |
| 1.26 mm to 1.65mm | 3 per 30 cm x 30 cm area |
| 1.66 mm to 2.54 mm | 1 per 30 cm x 30 cm area |
| - 2.54 mm | None |
| ## Black Specks |  |
| < 0.5 mm | Acceptable |
| 0.53 mm to 0.75 mm | 6 per 30 cm x 30 cm area |
| 0.76 mm to 1.65 mm | 3 per 30 cm x 30 cm area |
| 1.66 mm to 2.54 mm | 1 per 30 cm x 30 cm area |
| - 2.54 mm | None |
| ### Splatter, Voids, White Spots |  |
| < 0.5mm | Acceptable |
| 0.53 mm to 1.65 mm | 2 per 30 cm x 30 cm area |
| 1.66 mm to 2.54 mm | 1 per 30 cm x 30 cm area |
| - 2.54 mm | None |

*Visual Inspection

*There shall be no more than 1 cluster of defects on a sheet, and limited to 20% of the total sheet area, leaving a minimum of 80% usable sheet.

* 30 cm x 30 cm = 1 sq. ft. (approx.)